Supplementary materials for X-ray crystallographic data of anti-[Pd(-NH2)(Ph)(PEt3)]2 (1) (Tables 1-1 to 5-1) and [Pd(dppe)(NH2)]2(OTf)2 (2) (Tables 1-2 to 5-2): crystal data, atomic coordinates and equivalent isotropic displacement parameters, bond lengths and angles, anisotropic displacement parameters, hydrogen coordinates and isotropic displacement parameters.

Parent-amido (NH2) palladium(II) complexes: synthesis, reactions, and catalytic hydroamination

# Young Won Kim, Soonheum Park *

Department of Chemistry, Dongguk University-Gyeongju, 123 Dongdae-ro, Gyeongju, Gyeongbuk, Republic of Korea.

Table 1-1. Crystal data and structure refinement for anti-[Pd(-NH2)(Ph)(PEt3)]2 (1).

Chemical formula                  C24H44N2P2Pd2

Formula weight                    635.41

Temperature                       293(2) K

Wavelength                        0.71069 Å

Crystal system                    Monoclinic

Space group                       P21/n

Unit cell dimensions              a = 13.228(2) Å  α = 90.000(10) deg.

b = 18.132(2) Å  β = 101.410(10) deg.

c = 24.745(2) Å  γ = 90.000(10) deg.

Volume                            5817.8(12) Å3

Z                                 4

Density (calculated)              1.451 Mg/m3

Absorption coefficient            1.360 mm-1

F(000)                            2688

Crystal size                      0.80 x 0.50 x 0.25 mm

Theta range for data collection   2.02 to 22.56 deg.

Index ranges                      0≤h≤14, 0≤k≤19,

-26≤l≤26

Reflections collected             7990

Independent reflections           7614 [R(int) = 0.0373]

Refinement method                 Full-matrix least-squares on F2

Data / restraints / parameters    7613 / 0 / 540

Goodness-of-fit on F2              1.122

Final R indices [I>2(I)]a         R1 = 0.0547, wR2 = 0.1417

R indices (all data)a              R1 = 0.0715, wR2 = 0.1504

Largest diff. peak and hole        0.743 and -0.717 e Å-3

a R1 = Fo - Fc/Fo; wR2 = [w(Fo2 - Fc2)2/wFo4]1/2

Table 2-1. Atomic coordinates (×104) and equivalent isotropic displacement parameters (Å2×103) for 1. U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

______________________________________________________________________

x             y             z           U(eq)

______________________________________________________________________

Pd(1)        5994(1)       8523(1)      -2395(1)       58(1)

Pd(2)        7028(1)       8115(1)      -1262(1)       61(1)

P(1)         5088(2)       9536(2)      -2686(1)       73(1)

P(2)         6833(2)       7116(2)       -764(1)       76(1)

N(1)         7143(6)       8991(5)      -1781(3)       72(2)

N(2)         6803(6)       7595(4)      -2047(3)       67(2)

C(1)         4979(7)       7930(5)      -2929(3)       59(2)

C(2)         5199(7)       7649(6)      -3411(4)       69(3)

C(3)         4488(9)       7240(6)      -3781(4)       80(3)

C(4)         3539(9)       7082(6)      -3680(4)       82(3)

C(5)         3306(8)       7335(6)      -3198(4)       82(3)

C(6)         4010(8)       7743(6)      -2837(4)       77(3)

C(7)         5733(8)      10419(6)      -2548(5)       86(3)

C(8)         6697(11)     10516(7)      -2766(5)      106(4)

C(9)         3988(9)       9656(8)      -2358(6)      114(4)

C(10)        4252(13)      9569(9)      -1741(7)      139(6)

C(11)        4435(11)      9594(7)      -3408(5)      112(5)

C(12)        5108(16)      9538(10)     -3825(6)      158(7)

C(13)        7227(8)       8761(5)       -595(3)       63(2)

C(14)        6417(9)       9055(5)       -401(4)       79(3)

C(15)        6547(11)      9508(6)         68(5)       92(4)

C(16)        7509(14)      9653(8)        353(5)      105(4)

C(17)        8326(12)      9385(7)        173(5)      106(4)

C(18)        8196(9)       8930(6)       -282(4)       87(3)

C(19)        6769(13)      7269(8)        -39(5)      130(5)

C(20)        6667(15)      6552(9)        315(6)      152(6)

C(21)        7931(16)      6425(9)       -695(7)      160(7)

C(22)        8919(14)      6783(12)      -321(8)      179(8)

C(23)        5847(17)      6480(10)     -1090(7)      204(9)

C(24)        4732(13)      6999(13)     -1185(9)      206(10)

Pd(3)        4183(1)       6794(1)       2324(1)       54(1)

Pd(4)        3034(1)       7111(1)       1204(1)       54(1)

P(3)         5192(2)       5830(2)       2617(1)       69(1)

P(4)         3142(2)       8063(2)        644(1)       69(1)

N(3)         3011(5)       6261(4)       1764(3)       62(2)

N(4)         3300(6)       7682(4)       1968(3)       60(2)

C(31)        5214(7)       7448(5)       2795(4)       61(2)

C(32)        5069(8)       7713(6)       3304(4)       78(3)

C(33)        5794(11)      8171(7)       3628(5)       99(4)

C(34)        6656(10)      8377(7)       3452(6)      103(4)

C(35)        6804(9)       8152(7)       2958(5)      105(4)

C(36)        6079(8)       7697(6)       2635(4)       82(3)

C(37)        5836(9)       5805(7)       3337(4)       92(4)

C(38)        5100(12)      5764(8)       3745(5)      119(5)

C(39)        4560(9)       4942(6)       2523(5)       98(4)

C(40)        5198(14)      4251(8)       2688(7)      154(7)

C(41)        6254(9)       5750(8)       2272(5)      112(4)

C(42)        5964(15)      5741(11)      1656(7)      171(8)

C(43)        2847(8)       6411(6)        572(4)       67(3)

C(44)        3664(10)      6133(7)        366(5)      102(4)

C(45)        3535(14)      5616(8)        -70(6)      122(5)

C(46)        2581(18)      5378(8)       -292(6)      122(6)

C(47)        1755(13)      5638(8)       -106(5)      114(5)

C(48)        1898(9)       6156(6)        321(4)       87(3)

C(491)       4454(15)      8242(11)       534(9)      108(8)

C(492)       4190(28)      8652(21)       895(15)      83(16)

C(50)        5268(10)      8236(8)       1039(6)      117(5)

C(511)       2853(14)      8980(10)       916(7)       83(7)

C(512)       1958(28)      8667(21)       513(16)     109(15)

C(52)        1779(12)      9036(9)       1078(8)      145(6)

C(531)       2332(18)      8060(11)       -54(8)       81(7)

C(541)       1225(24)      8065(16)       -30(13)     137(11)

C(532)       3060(25)      7776(17)      -140(13)     113(11)

C(542)       3115(29)      8389(21)      -517(16)     150(15)

______________________________________________________________________

Table 3-1. Bond lengths [Å] and angles [°] for 1.

________________________________________________

Pd(1)-C(1)      2.000(9)

Pd(1)-N(2)      2.085(7)

Pd(1)-N(1)      2.104(7)

Pd(1)-P(1)      2.233(3)

Pd(2)-C(13)     1.998(9)

Pd(2)-N(1)      2.067(7)

Pd(2)-N(2)      2.127(7)

Pd(2)-P(2)      2.235(3)

P(1)-C(7)       1.814(11)

P(1)-C(9)       1.813(13)

P(1)-C(11)      1.827(12)

P(2)-C(23)      1.81(2)

P(2)-C(19)      1.832(12)

P(2)-C(21)      1.90(2)

C(1)-C(2)       1.382(12)

C(1)-C(6)       1.387(13)

C(2)-C(3)       1.389(13)

C(3)-C(4)       1.357(14)

C(4)-C(5)       1.368(14)

C(5)-C(6)       1.373(13)

C(7)-C(8)       1.49(2)

C(9)-C(10)      1.51(2)

C(11)-C(12)     1.49(2)

C(13)-C(14)     1.365(14)

C(13)-C(18)     1.395(13)

C(14)-C(15)     1.41(2)

C(15)-C(16)     1.35(2)

C(16)-C(17)     1.34(2)

C(17)-C(18)     1.38(2)

C(19)-C(20)     1.59(2)

C(21)-C(22)     1.58(2)

C(23)-C(24)     1.73(3)

Pd(3)-C(31)     1.998(9)

Pd(3)-N(4)      2.080(7)

Pd(3)-N(3)      2.100(7)

Pd(3)-P(3)      2.231(3)

Pd(4)-C(43)     1.992(10)

Pd(4)-N(3)      2.076(7)

Pd(4)-N(4)      2.122(7)

Pd(4)-P(4)      2.236(3)

P(3)-C(41)      1.789(12)

P(3)-C(39)      1.808(11)

P(3)-C(37)      1.817(10)

P(4)-C(492)     1.76(4)

P(4)-C(491)     1.84(2)

P(4)-C(531)     1.85(2)

P(4)-C(511)     1.86(2)

P(4)-C(512)     1.89(4)

P(4)-C(532)     1.99(3)

C(31)-C(36)     1.359(13)

C(31)-C(32)     1.397(12)

C(32)-C(33)     1.39(2)

C(33)-C(34)     1.35(2)

C(34)-C(35)     1.34(2)

C(35)-C(36)     1.390(14)

C(37)-C(38)     1.54(2)

C(39)-C(40)     1.52(2)

C(41)-C(42)     1.50(2)

C(43)-C(48)     1.367(13)

C(43)-C(44)     1.38(2)

C(44)-C(45)     1.42(2)

C(45)-C(46)     1.34(2)

C(46)-C(47)     1.35(2)

C(47)-C(48)     1.40(2)

C(491)-C(492)   1.26(4)

C(491)-C(50)    1.48(2)

C(492)-C(50)    1.59(4)

C(492)-C(511)   1.88(4)

C(511)-C(512)   1.50(4)

C(511)-C(52)    1.55(2)

C(512)-C(52)    1.61(4)

C(512)-C(541)   1.85(5)

C(512)-C(531)   1.92(4)

C(531)-C(532)   1.15(3)

C(531)-C(541)   1.48(3)

C(531)-C(542)   1.79(4)

C(532)-C(542)   1.46(4)

C(1)-Pd(1)-N(2)          93.5(3)

C(1)-Pd(1)-N(1)          171.3(3)

N(2)-Pd(1)-N(1)           77.8(3)

C(1)-Pd(1)-P(1)           89.0(3)

N(2)-Pd(1)-P(1)          174.3(2)

N(1)-Pd(1)-P(1)           99.5(2)

C(1)-Pd(1)-Pd(2)         128.0(3)

N(2)-Pd(1)-Pd(2)          45.9(2)

N(1)-Pd(1)-Pd(2)          44.3(2)

P(1)-Pd(1)-Pd(2)         128.94(8)

C(13)-Pd(2)-N(1)         92.8(3)

C(13)-Pd(2)-N(2)        170.4(3)

N(1)-Pd(2)-N(2)          77.7(3)

C(13)-Pd(2)-P(2)         91.7(3)

N(1)-Pd(2)-P(2)         175.1(2)

N(2)-Pd(2)-P(2)          97.7(2)

C(13)-Pd(2)-Pd(1)       126.6(3)

N(1)-Pd(2)-Pd(1)         45.3(2)

N(2)-Pd(2)-Pd(1)         44.8(2)

P(2)-Pd(2)-Pd(1)        130.02(8)

C(7)-P(1)-C(9)          101.5(6)

C(7)-P(1)-C(11)         104.2(6)

C(9)-P(1)-C(11)          99.4(7)

C(7)-P(1)-Pd(1)         117.6(4)

C(9)-P(1)-Pd(1)         112.5(5)

C(11)-P(1)-Pd(1)        118.8(4)

C(23)-P(2)-C(19)        111.4(8)

C(23)-P(2)-C(21)         95.2(10)

C(19)-P(2)-C(21)        101.2(7)

C(23)-P(2)-Pd(2)        115.0(6)

C(19)-P(2)-Pd(2)        116.7(5)

C(21)-P(2)-Pd(2)        114.5(5)

Pd(2)-N(1)-Pd(1)         90.4(3)

Pd(1)-N(2)-Pd(2)         89.3(3)

C(2)-C(1)-C(6)          114.2(9)

C(2)-C(1)-Pd(1)         122.7(7)

C(6)-C(1)-Pd(1)         123.0(7)

C(1)-C(2)-C(3)          122.3(9)

C(4)-C(3)-C(2)          121.5(9)

C(3)-C(4)-C(5)          117.7(10)

C(4)-C(5)-C(6)          120.4(10)

C(5)-C(6)-C(1)          123.7(9)

C(8)-C(7)-P(1)          116.2(8)

C(10)-C(9)-P(1)         113.3(9)

C(12)-C(11)-P(1)        116.1(10)

C(14)-C(13)-C(18)       114.8(10)

C(14)-C(13)-Pd(2)       122.3(8)

C(18)-C(13)-Pd(2)       122.9(9)

C(13)-C(14)-C(15)       122.8(11)

C(16)-C(15)-C(14)       119.6(13)

C(17)-C(16)-C(15)       119.6(12)

C(16)-C(17)-C(18)       120.7(13)

C(17)-C(18)-C(13)       122.5(12)

C(20)-C(19)-P(2)        116.2(10)

C(22)-C(21)-P(2)        108.0(12)

C(24)-C(23)-P(2)        103.5(12)

C(31)-Pd(3)-N(4)         92.8(3)

C(31)-Pd(3)-N(3)        171.0(3)

N(4)-Pd(3)-N(3)          78.3(3)

C(31)-Pd(3)-P(3)         88.8(3)

N(4)-Pd(3)-P(3)         173.6(2)

N(3)-Pd(3)-P(3)          99.8(2)

C(31)-Pd(3)-Pd(4)       126.8(3)

N(4)-Pd(3)-Pd(4)         46.2(2)

N(3)-Pd(3)-Pd(4)         44.9(2)

P(3)-Pd(3)-Pd(4)        128.61(8)

C(43)-Pd(4)-N(3)        92.0(3)

C(43)-Pd(4)-N(4)       169.6(3)

N(3)-Pd(4)-N(4)         77.9(3)

C(43)-Pd(4)-P(4)        91.0(3)

N(3)-Pd(4)-P(4)        176.1(2)

N(4)-Pd(4)-P(4)         98.9(2)

C(43)-Pd(4)-Pd(3)      125.2(3)

N(3)-Pd(4)-Pd(3)        45.6(2)

N(4)-Pd(4)-Pd(3)        45.0(2)

P(4)-Pd(4)-Pd(3)       130.55(8)

C(41)-P(3)-C(39)       104.7(7)

C(41)-P(3)-C(37)       101.9(6)

C(39)-P(3)-C(37)       102.7(5)

C(41)-P(3)-Pd(3)       112.6(4)

C(39)-P(3)-Pd(3)       115.1(4)

C(37)-P(3)-Pd(3)       118.2(4)

C(492)-P(4)-C(491)      41.0(12)

C(492)-P(4)-C(531)     127.1(13)

C(491)-P(4)-C(531)     104.6(10)

C(492)-P(4)-C(511)      62.3(14)

C(491)-P(4)-C(511)      99.5(9)

C(531)-P(4)-C(511)     102.6(9)

C(492)-P(4)-C(512)     106(2)

C(491)-P(4)-C(512)     130.4(13)

C(531)-P(4)-C(512)      62.1(14)

C(511)-P(4)-C(512)      47.2(12)

C(492)-P(4)-C(532)     113(2)

C(491)-P(4)-C(532)      76.8(11)

C(531)-P(4)-C(532)      34.5(9)

C(511)-P(4)-C(532)     127.6(11)

C(512)-P(4)-C(532)      96(2)

C(492)-P(4)-Pd(4)      113.1(12)

C(491)-P(4)-Pd(4)      114.0(6)

C(531)-P(4)-Pd(4)      118.8(6)

C(511)-P(4)-Pd(4)      115.0(5)

C(512)-P(4)-Pd(4)      113.7(11)

C(532)-P(4)-Pd(4)      113.8(9)

Pd(4)-N(3)-Pd(3)        89.5(3)

Pd(3)-N(4)-Pd(4)        88.8(3)

C(36)-C(31)-C(32)      114.9(9)

C(36)-C(31)-Pd(3)      123.0(7)

C(32)-C(31)-Pd(3)      122.1(7)

C(33)-C(32)-C(31)      121.4(11)

C(34)-C(33)-C(32)      120.5(11)

C(35)-C(34)-C(33)      119.6(11)

C(34)-C(35)-C(36)      119.7(12)

C(31)-C(36)-C(35)      123.7(10)

C(38)-C(37)-P(3)       114.2(8)

C(40)-C(39)-P(3)       118.7(10)

C(42)-C(41)-P(3)       114.8(10)

C(48)-C(43)-C(44)      115.1(10)

C(48)-C(43)-Pd(4)      122.2(9)

C(44)-C(43)-Pd(4)      122.6(8)

C(43)-C(44)-C(45)      122.7(13)

C(46)-C(45)-C(44)      119(2)

C(45)-C(46)-C(47)      120(2)

C(46)-C(47)-C(48)      119.6(14)

C(43)-C(48)-C(47)      123.1(13)

C(492)-C(491)-C(50)     70(2)

C(492)-C(491)-P(4)      66(2)

C(50)-C(491)-P(4)      115.0(13)

C(491)-C(492)-C(50)     61(2)

C(491)-C(492)-P(4)      73(2)

C(50)-C(492)-P(4)      114(2)

C(491)-C(492)-C(511)   127(3)

C(50)-C(492)-C(511)    162(3)

P(4)-C(492)-C(511)      61.4(13)

C(491)-C(50)-C(492)     48.5(14)

C(512)-C(511)-C(52)     64(2)

C(512)-C(511)-P(4)      67(2)

C(52)-C(511)-P(4)      114.6(12)

C(512)-C(511)-C(492)   119(2)

C(52)-C(511)-C(492)    161(2)

P(4)-C(511)-C(492)      56.3(13)

C(511)-C(512)-C(52)     60(2)

C(511)-C(512)-C(541)   160(3)

C(52)-C(512)-C(541)    137(3)

C(511)-C(512)-P(4)      66(2)

C(52)-C(512)-P(4)      111(2)

C(541)-C(512)-P(4)      95(2)

C(511)-C(512)-C(531)   115(2)

C(52)-C(512)-C(531)    167(3)

C(541)-C(512)-C(531)    46.0(14)

P(4)-C(512)-C(531)      57.9(13)

C(511)-C(52)-C(512)     57(2)

C(532)-C(531)-C(541)   152(3)

C(532)-C(531)-C(542)    55(2)

C(541)-C(531)-C(542)   137(2)

C(532)-C(531)-P(4)      80(2)

C(541)-C(531)-P(4)     111(2)

C(542)-C(531)-P(4)     107(2)

C(532)-C(531)-C(512)   137(3)

C(541)-C(531)-C(512)    64(2)

C(542)-C(531)-C(512)   123(2)

P(4)-C(531)-C(512)      60.0(13)

C(531)-C(541)-C(512)    70(2)

C(531)-C(532)-C(542)    86(3)

C(531)-C(532)-P(4)      66(2)

C(542)-C(532)-P(4)     115(2)

C(532)-C(542)-C(531)    40(2)

___________________________________________________________

Symmetry transformations used to generate equivalent atoms:

Table 4-1. Anisotropic displacement parameters (Å2×103) for 1. The anisotropic displacement factor exponent takes the form: -22[h2a*2U11 +  + 2hka*b*U12].

___________________________________________________________________________

U11        U22         U33         U23        U13         U12

___________________________________________________________________________

Pd(1)    55(1)      74(1)      43(1)      -2(1)       4(1)       0(1)

Pd(2)    60(1)      76(1)      44(1)       1(1)       5(1)      -3(1)

P(1)     67(2)      78(2)      67(2)      -4(1)      -2(1)       4(1)

P(2)     95(2)      74(2)      59(2)       1(1)      17(1)      -3(2)

N(1)     68(5)      92(6)      50(4)       9(4)      -3(4)     -17(4)

N(2)     61(5)      81(6)      59(5)      -5(4)       8(4)       8(4)

C(1)     62(6)      72(6)      44(5)       4(4)       9(4)       4(5)

C(2)     60(6)      89(7)      56(6)      -4(5)       8(5)       7(5)

C(3)     92(8)      97(8)      47(6)     -24(6)       4(5)       5(7)

C(4)     75(7)      92(8)      66(7)     -12(6)     -13(6)      -9(6)

C(5)     62(6)      99(8)      86(8)     -20(7)      15(6)      -4(6)

C(6)     80(7)      94(8)      60(6)     -17(6)      20(5)      -5(6)

C(7)     84(8)      89(8)      81(8)      -9(6)      12(6)       7(6)

C(8)    129(11)     91(9)     105(10)     -8(7)      36(8)      -9(8)

C(9)     74(8)     120(11)    149(13)     -1(10)     22(8)      11(7)

C(10)   138(13)    149(14)    153(15)    -27(12)     82(12)      1(11)

C(11)   127(11)     85(9)     104(10)      7(8)     -27(9)      28(8)

C(12)   226(20)    156(15)     72(9)      29(10)    -15(11)     37(14)

C(13)    88(7)      62(6)      35(5)       3(4)       2(5)     -11(5)

C(14)   100(8)      62(7)      76(7)      -7(6)      18(6)     -12(6)

C(15)   133(11)     65(7)      84(8)       5(7)      32(8)       9(7)

C(16)   160(14)    106(11)     42(6)      -3(6)      -2(8)     -10(10)

C(17)   132(12)    102(11)     70(8)      -5(7)     -13(8)     -33(9)

C(18)    81(8)      97(9)      73(7)       7(7)      -7(6)     -13(6)

C(19)   228(17)    105(10)     70(8)      14(7)      60(9)     -15(11)

C(20)   235(19)    124(12)    111(11)     39(10)     71(12)      6(12)

C(21)   243(19)    117(12)    139(13)     25(10)     82(14)     60(13)

C(22)   126(13)    236(22)    162(17)     54(16)     -1(12)     22(14)

C(23)   299(22)    153(15)    131(12)     23(11)    -28(13)   -128(15)

C(24)    94(11)    296(26)    214(22)     89(20)     -4(13)    -46(14)

Pd(3)    51(1)      68(1)      41(1)       3(1)       5(1)      -1(1)

Pd(4)    56(1)      61(1)      42(1)       4(1)       3(1)      -2(1)

P(3)     58(2)      81(2)      61(2)      10(1)      -1(1)       8(1)

P(4)     79(2)      71(2)      55(2)      12(1)      10(1)      -4(1)

N(3)     56(4)      70(5)      56(4)      15(4)       4(3)      -8(4)

N(4)     69(5)      58(5)      55(4)       1(4)      16(4)       7(4)

C(31)    50(5)      80(7)      51(5)      -7(5)       0(4)       0(5)

C(32)    85(7)      88(8)      60(6)      -9(6)      14(5)       0(6)

C(33)   121(11)    106(10)     61(7)     -30(7)      -1(7)      12(8)

C(34)    77(8)     106(10)    113(11)    -47(8)     -16(8)      -3(7)

C(35)    79(8)     129(11)    106(10)    -42(9)      16(7)     -17(7)

C(36)    70(7)     110(9)      67(7)     -28(6)      14(5)     -21(6)

C(37)    91(8)      95(9)      73(7)      22(6)     -27(6)       4(7)

C(38)   137(12)    131(12)     83(9)      37(8)      10(8)       0(9)

C(39)   109(9)      81(8)      90(8)      -6(7)     -10(7)       0(7)

C(40)   181(16)     86(10)    162(15)      2(10)    -44(12)     30(10)

C(41)    94(9)     143(12)    104(10)     22(9)      30(8)      35(8)

C(42)   189(17)    226(20)    121(13)     32(13)     88(13)     79(15)

C(43)    79(7)      74(7)      42(5)       7(5)      -5(5)       0(6)

C(44)   110(10)    109(10)     84(8)     -23(8)      10(7)       8(8)

C(45)   154(15)    119(12)     90(10)    -18(9)      18(10)     37(11)

C(46)   197(19)     75(10)     79(10)     -1(7)     -12(12)     19(11)

C(47)   142(13)     95(11)     76(9)       8(8)     -47(9)     -20(9)

C(48)   101(9)      85(8)      64(7)      -1(6)     -11(6)     -16(7)

C(50)    90(9)     146(12)    113(11)      2(9)      14(8)     -28(9)

C(52)   126(12)    118(12)    202(18)     23(12)     59(12)     37(10)

______________________________________________________________________________

Table 5-1. Hydrogen coordinates (×104) and isotropic displacement parameters (Å2×103) for 1.

_________________________________________________________________________

x            y             z           U(eq)

_________________________________________________________________________

H(1A)        7763(6)       9024(5)      -1878(3)       87

H(1B)        6961(6)       9426(5)      -1654(3)       87

H(2A)        7391(6)       7513(4)      -2168(3)       81

H(2B)        6416(6)       7184(4)      -2071(3)       81

H(2)         5846(7)       7736(6)      -3492(4)       83

H(3)         4665(9)       7071(6)      -4104(4)       96

H(4)         3064(9)       6812(6)      -3930(4)       98

H(5)         2666(8)       7229(6)      -3115(4)       99

H(6)         3827(8)       7904(6)      -2513(4)       93

H(7A)        5252(8)      10803(6)      -2704(5)      103

H(7B)        5896(8)      10492(6)      -2152(5)      103

H(8A)        6975         10998         -2671         128

H(8B)        6546         10463         -3160         128

H(8C)        7191         10149         -2607         128

H(9A)        3700(9)      10143(8)      -2446(6)      137

H(9B)        3463(9)       9298(8)      -2509(6)      137

H(10A)       3642          9639         -1591         167

H(10B)       4760          9929         -1588         167

H(10C)       4521          9083         -1651         167

H(11A)       3925(11)      9204(7)      -3479(5)      135

H(11B)       4068(11)     10060(7)      -3462(5)      135

H(12A)       4692          9575         -4188         189

H(12B)       5461          9073         -3785         189

H(12C)       5604          9931         -3768         189

H(14)        5751(9)       8950(5)       -588(4)       95

H(15)        5976(11)      9708(6)        182(5)      111

H(16)        7602(14)      9936(8)        673(5)      126

H(17)        8988(12)      9508(7)        357(5)      127

H(18)        8777(9)       8728(6)       -384(4)      104

H(3A)        3201(5)       5821(4)       1647(3)       74

H(3B)        2412(5)       6224(4)       1882(3)       74

H(4A)        3660(6)       8103(4)       1966(3)       72

H(4B)        2726(6)       7758(4)       2104(3)       72

H(32)        4476(8)       7582(6)       3430(4)       93

H(33)        5683(11)      8335(7)       3967(5)      119

H(34)        7144(10)      8673(7)       3673(6)      124

H(35)        7389(9)       8299(7)       2831(5)      126

H(36)        6192(8)       7556(6)       2291(4)       99

H(37A)       6291(9)       5381(7)       3394(4)      111

H(37B)       6260(9)       6243(7)       3417(4)      111

H(38A)       5494          5752          4115         143

H(38B)       4689          5325          3676         143

H(38C)       4658          6189          3699         143

H(39A)       4006(9)       4947(6)       2728(5)      117

H(39B)       4242(9)       4896(6)       2136(5)      117

H(40A)       4763          3825          2615       184

H(40B)       5498          4272          3074       184

H(40C)       5735          4221          2479       184

H(41A)       6721(9)       6159(8)       2383(5)    135

H(41B)       6626(9)       5299(8)       2393(5)    135

H(42A)       6575          5695          1504       205

H(42B)       5615          6192          1529       205

H(42C)       5515          5331          1539       205

H(44)        4327(10)      6291(7)        521(5)    123

H(45)        4102(14)      5443(8)       -202(6)    146

H(46)        2488(18)      5032(8)       -576(6)    147

H(47)        1095(13)      5473(8)       -260(5)    137

H(48)        1320(9)       6336(6)        439(4)    105

_________________________________________________________________________

Table 1-2. Crystal data and structure refinement for [Pd(dppe)(-NH2)]2(OTf)2 (2).

Chemical formula                  C54H52F6N2O6P4Pd2S2

Formula weight                    1339.78

Temperature                       293(2) K

Wavelength                        0.71069 Å

Crystal system                    Monoclinic

Space group                       P21/n

Unit cell dimensions              a = 11.4478(7) Å  α = 90.000(8) deg.

b = 43.540(3) Å  β = 104.127(6) deg.

c = 11.7208(8) Å  γ = 90.000(6) deg.

Volume                            5665.4(6) Å3

Z                                 4

Density (calculated)              1.571 Mg/m3

Absorption coefficient            0.891 mm-1

F(000)                            2704

Crystal size                      0.66 x 0.32 x 0.18 mm

Theta range for data collection   1.85 to 22.47 deg.

Index ranges                      0≤h≤12, 0≤k≤46, -12≤l≤12

Reflections collected             7812

Independent reflections           7390 [R(int) = 0.0223]

Refinement method                 Full-matrix least-squares on F2

Data / restraints / parameters    7390 / 0 / 685

Goodness-of-fit on F2              1.220

Final R indices [I>2(I)]a         R1 = 0.0502, wR2 = 0.1260

R indices (all data)a              R1 = 0.0593, wR2 = 0.1300

Largest diff. peak and hole        0.493 and -0.487 e Å-3

a R1 = Fo - Fc/Fo; wR2 = [w(Fo2 - Fc2)2/wFo4]1/2

Table 2-2. Atomic coordinates (×104) and equivalent isotropic displacement parameters (Å2×103) for 2. U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

_______________________________________________________________

x             y             z           U(eq)

_______________________________________________________________

Pd(1)        9269(1)       1159(1)       -817(1)       33(1)

Pd(2)        9446(1)       1414(1)       1659(1)       35(1)

P(1)         7824(2)       1026(1)      -2419(2)       36(1)

P(2)        10452(2)        832(1)      -1493(2)       39(1)

P(3)         8224(2)       1609(1)       2704(2)       42(1)

P(4)        10720(2)       1365(1)       3438(2)       47(1)

N(1)         8343(5)       1473(2)        -11(5)       43(2)

N(2)        10608(5)       1276(2)        648(5)       41(2)

C(1)         7004(7)       1336(2)      -3287(7)       41(2)

C(2)         7320(8)       1637(2)      -3006(8)       56(2)

C(3)         6753(10)      1881(2)      -3682(8)       66(3)

C(4)         5874(8)       1820(2)      -4671(9)       64(3)

C(5)         5567(8)       1528(2)      -4974(9)       69(3)

C(6)         6106(7)       1279(2)      -4305(8)       57(2)

C(7)         6741(7)        756(2)      -2104(7)       41(2)

C(8)         6564(8)        739(2)       -976(8)       53(2)

C(9)         5754(9)        545(2)       -691(9)       67(3)

C(10)        5113(8)        346(2)      -1549(10)      65(3)

C(11)        5275(8)        351(2)      -2657(10)      61(3)

C(12)        6086(7)        552(2)      -2942(8)       49(2)

C(13)        8565(7)        823(2)      -3407(7)       46(2)

C(14)        9504(7)        607(2)      -2680(7)       49(2)

C(15)       11201(7)        566(2)       -370(7)       42(2)

C(16)       10524(9)        426(2)        300(9)       65(3)

C(17)       11047(10)       219(3)       1183(10)      81(3)

C(18)       12249(10)       161(2)       1425(10)      77(3)

C(19)       12938(10)       315(3)        786(10)      85(3)

C(20)       12434(8)        512(2)        -95(9)       68(3)

C(21)       11599(7)       1012(2)      -2080(7)       44(2)

C(22)       12248(8)        853(2)      -2755(8)       60(2)

C(23)       13176(9)        994(3)      -3106(9)       76(3)

C(24)       13487(9)       1299(3)      -2790(10)      76(3)

C(25)       12852(10)      1457(2)      -2141(9)       74(3)

C(26)       11896(8)       1317(2)      -1798(8)       59(2)

C(27)        6614(7)       1571(2)       2089(7)       47(2)

C(28)        5873(9)       1832(2)       1851(9)       68(3)

C(29)        4659(10)      1794(3)       1327(12)      92(4)

C(30)        4206(10)      1504(3)       1094(10)      84(3)

C(31)        4924(10)      1253(3)       1321(11)      90(4)

C(32)        6138(8)       1296(2)       1823(9)       68(3)

C(33)        8598(7)       2008(2)       3012(7)       46(2)

C(34)        9127(9)       2175(2)       2270(9)       66(3)

C(35)        9546(10)      2463(2)       2546(12)      84(3)

C(36)        9429(11)      2602(3)       3551(12)      87(4)

C(37)        8876(12)      2447(3)       4300(12)      97(4)

C(38)        8460(10)      2154(3)       4026(9)       79(3)

C(39)        8553(7)       1408(2)       4117(7)       53(2)

C(40)        9847(8)       1351(4)       4571(8)      100(5)

C(41)       11661(7)       1705(2)       3774(7)       48(2)

C(42)       11966(9)       1864(3)       2895(9)       75(3)

C(43)       12606(10)      2138(3)       3107(11)      86(3)

C(44)       12942(11)      2244(3)       4204(15)      97(4)

C(45)       12653(14)      2092(4)       5085(14)     124(5)

C(46)       12033(11)      1818(3)       4890(10)      92(4)

C(47)       11711(8)       1035(2)       3670(7)       53(2)

C(48)       11342(12)       756(3)       4027(10)      90(4)

C(49)       12094(19)       502(3)       4203(13)     120(5)

C(50)       13228(17)       529(4)       4051(13)     118(6)

C(51)       13607(11)       805(3)       3684(11)      97(4)

C(52)       12846(8)       1053(2)       3475(9)       67(3)

S(1)        10694(2)       2142(1)       -583(2)       62(1)

O(1)        10998(7)       2440(2)       -121(7)       93(2)

O(2)        11598(7)       1916(2)       -256(6)       87(2)

O(3)         9512(7)       2045(2)       -535(7)       98(3)

C(53)       10509(11)      2193(3)      -2151(10)      76(3)

F(1)        10180(7)       1934(2)      -2731(6)      111(2)

F(2)        11496(8)       2276(2)      -2427(7)      141(3)

F(3)         9688(8)       2397(2)      -2593(7)      140(3)

S(2)         6941(3)        429(1)       3419(3)       87(1)

O(4)         6026(8)        419(2)       2359(7)      114(3)

O(5)         6714(11)       245(3)       4361(9)      158(4)

O(6)         7390(13)       713(2)       3782(9)      184(6)

C(54)        8103(14)       216(4)       3133(24)     150(7)

F(4)         9044(10)       216(3)       3998(16)     254(8)

F(5)         7818(12)       -57(3)       2762(15)     254(8)

F(6)         8472(13)       369(5)       2265(15)     271(9)

_______________________________________________________________

Table 3-2. Bond lengths [Å] and angles [°] for 2.

_____________________________________________________________

Pd(1)-N(2)                    2.067(6)

Pd(1)-N(1)                    2.089(6)

Pd(1)-P(2)                    2.240(2)

Pd(1)-P(1)                    2.255(2)

Pd(1)-Pd(2)                   3.0669(8)

Pd(2)-N(1)                    2.069(6)

Pd(2)-N(2)                    2.075(6)

Pd(2)-P(3)                    2.240(2)

Pd(2)-P(4)                    2.244(2)

P(1)-C(7)                     1.809(8)

P(1)-C(1)                     1.811(8)

P(1)-C(13)                    1.821(8)

P(2)-C(21)                    1.804(8)

P(2)-C(15)                    1.807(8)

P(2)-C(14)                    1.827(8)

P(3)-C(33)                    1.802(8)

P(3)-C(27)                    1.815(8)

P(3)-C(39)                    1.830(8)

P(4)-C(47)                    1.811(9)

P(4)-C(41)                    1.816(9)

P(4)-C(40)                    1.847(9)

C(1)-C(2)                     1.377(11)

C(1)-C(6)                     1.394(11)

C(2)-C(3)                     1.388(12)

C(3)-C(4)                     1.364(13)

C(4)-C(5)                     1.344(13)

C(5)-C(6)                     1.391(12)

C(7)-C(8)                     1.388(11)

C(7)-C(12)                    1.398(11)

C(8)-C(9)                     1.356(12)

C(9)-C(10)                    1.392(13)

C(10)-C(11)                   1.356(13)

C(11)-C(12)                   1.376(12)

C(13)-C(14)                   1.524(11)

C(15)-C(16)                   1.373(12)

C(15)-C(20)                   1.388(11)

C(16)-C(17)                   1.393(13)

C(17)-C(18)                   1.359(14)

C(18)-C(19)                   1.387(14)

C(19)-C(20)                   1.359(13)

C(21)-C(26)                   1.389(12)

C(21)-C(22)                   1.395(11)

C(22)-C(23)                   1.374(13)

C(23)-C(24)                   1.40(2)

C(24)-C(25)                   1.360(14)

C(25)-C(26)                   1.394(12)

C(27)-C(32)                   1.322(12)

C(27)-C(28)                   1.405(12)

C(28)-C(29)                   1.386(14)

C(29)-C(30)                   1.37(2)

C(30)-C(31)                   1.36(2)

C(31)-C(32)                   1.384(13)

C(33)-C(34)                   1.382(12)

C(33)-C(38)                   1.391(12)

C(34)-C(35)                   1.354(14)

C(35)-C(36)                   1.36(2)

C(36)-C(37)                   1.38(2)

C(37)-C(38)                   1.37(2)

C(39)-C(40)                   1.467(12)

C(41)-C(42)                   1.356(13)

C(41)-C(46)                   1.364(13)

C(42)-C(43)                   1.391(14)

C(43)-C(44)                   1.33(2)

C(44)-C(45)                   1.34(2)

C(45)-C(46)                   1.38(2)

C(47)-C(52)                   1.376(13)

C(47)-C(48)                   1.382(14)

C(48)-C(49)                   1.39(2)

C(49)-C(50)                   1.36(2)

C(50)-C(51)                   1.38(2)

C(51)-C(52)                   1.37(2)

S(1)-O(2)                     1.413(7)

S(1)-O(1)                     1.417(7)

S(1)-O(3)                     1.432(8)

S(1)-C(53)                    1.812(11)

C(53)-F(2)                    1.300(12)

C(53)-F(3)                    1.304(12)

C(53)-F(1)                    1.322(12)

S(2)-O(6)                     1.370(9)

S(2)-O(4)                     1.416(8)

S(2)-O(5)                     1.436(10)

S(2)-C(54)                    1.72(2)

C(54)-F(5)                    1.28(2)

C(54)-F(4)                    1.29(2)

C(54)-F(6)                    1.37(2)

N(2)-Pd(1)-N(1)              79.6(2)

N(2)-Pd(1)-P(2)              93.4(2)

N(1)-Pd(1)-P(2)             173.0(2)

N(2)-Pd(1)-P(1)             179.1(2)

N(1)-Pd(1)-P(1)             101.3(2)

P(2)-Pd(1)-P(1)              85.69(7)

N(2)-Pd(1)-Pd(2)             42.3(2)

N(1)-Pd(1)-Pd(2)             42.2(2)

P(2)-Pd(1)-Pd(2)            131.22(6)

P(1)-Pd(1)-Pd(2)            138.34(6)

N(1)-Pd(2)-N(2)              79.9(2)

N(1)-Pd(2)-P(3)              98.8(2)

N(2)-Pd(2)-P(3)             174.6(2)

N(1)-Pd(2)-P(4)             176.9(2)

N(2)-Pd(2)-P(4)              98.1(2)

P(3)-Pd(2)-P(4)              83.03(8)

N(1)-Pd(2)-Pd(1)             42.7(2)

N(2)-Pd(2)-Pd(1)             42.1(2)

P(3)-Pd(2)-Pd(1)            138.50(6)

P(4)-Pd(2)-Pd(1)            136.27(6)

C(7)-P(1)-C(1)              108.2(3)

C(7)-P(1)-C(13)             105.3(4)

C(1)-P(1)-C(13)             105.2(4)

C(7)-P(1)-Pd(1)             113.4(3)

C(1)-P(1)-Pd(1)             116.7(3)

C(13)-P(1)-Pd(1)            107.1(3)

C(21)-P(2)-C(15)            107.3(4)

C(21)-P(2)-C(14)            107.2(4)

C(15)-P(2)-C(14)            107.3(4)

C(21)-P(2)-Pd(1)            114.7(3)

C(15)-P(2)-Pd(1)            111.8(3)

C(14)-P(2)-Pd(1)            108.3(3)

C(33)-P(3)-C(27)            109.6(4)

C(33)-P(3)-C(39)            107.1(4)

C(27)-P(3)-C(39)            106.3(4)

C(33)-P(3)-Pd(2)            108.9(3)

C(27)-P(3)-Pd(2)            117.2(3)

C(39)-P(3)-Pd(2)            107.2(3)

C(47)-P(4)-C(41)            107.3(4)

C(47)-P(4)-C(40)            107.1(5)

C(41)-P(4)-C(40)            105.5(5)

C(47)-P(4)-Pd(2)            117.2(3)

C(41)-P(4)-Pd(2)            109.9(3)

C(40)-P(4)-Pd(2)            109.2(3)

Pd(2)-N(1)-Pd(1)             95.0(2)

Pd(1)-N(2)-Pd(2)             95.6(2)

C(2)-C(1)-C(6)              118.1(8)

C(2)-C(1)-P(1)              120.5(6)

C(6)-C(1)-P(1)              121.2(6)

C(1)-C(2)-C(3)              122.2(8)

C(4)-C(3)-C(2)              118.7(9)

C(5)-C(4)-C(3)              120.0(9)

C(4)-C(5)-C(6)              122.5(9)

C(5)-C(6)-C(1)              118.4(9)

C(8)-C(7)-C(12)             117.2(7)

C(8)-C(7)-P(1)              119.8(6)

C(12)-C(7)-P(1)             123.0(6)

C(9)-C(8)-C(7)              122.4(9)

C(8)-C(9)-C(10)             118.8(9)

C(11)-C(10)-C(9)            120.7(9)

C(10)-C(11)-C(12)           120.1(9)

C(11)-C(12)-C(7)            120.8(9)

C(14)-C(13)-P(1)            108.6(5)

C(13)-C(14)-P(2)            107.5(6)

C(16)-C(15)-C(20)           118.5(8)

C(16)-C(15)-P(2)            117.8(6)

C(20)-C(15)-P(2)            123.5(7)

C(15)-C(16)-C(17)           120.7(9)

C(18)-C(17)-C(16)           120.4(10)

C(17)-C(18)-C(19)           118.5(9)

C(20)-C(19)-C(18)           121.6(10)

C(19)-C(20)-C(15)           120.1(10)

C(26)-C(21)-C(22)           118.5(8)

C(26)-C(21)-P(2)            118.9(6)

C(22)-C(21)-P(2)            122.5(7)

C(23)-C(22)-C(21)           120.3(9)

C(22)-C(23)-C(24)           120.6(9)

C(25)-C(24)-C(23)           119.4(9)

C(24)-C(25)-C(26)           120.4(10)

C(21)-C(26)-C(25)           120.8(9)

C(32)-C(27)-C(28)           119.5(9)

C(32)-C(27)-P(3)            119.7(7)

C(28)-C(27)-P(3)            120.7(7)

C(29)-C(28)-C(27)           118.8(10)

C(30)-C(29)-C(28)           119.4(11)

C(31)-C(30)-C(29)           121.6(10)

C(30)-C(31)-C(32)           118.1(11)

C(27)-C(32)-C(31)           122.5(10)

C(34)-C(33)-C(38)           117.1(9)

C(34)-C(33)-P(3)            120.1(7)

C(38)-C(33)-P(3)            122.7(7)

C(35)-C(34)-C(33)           121.5(10)

C(34)-C(35)-C(36)           121.0(11)

C(35)-C(36)-C(37)           119.6(11)

C(38)-C(37)-C(36)           119.5(11)

C(37)-C(38)-C(33)           121.3(11)

C(40)-C(39)-P(3)            112.0(6)

C(39)-C(40)-P(4)            114.2(6)

C(42)-C(41)-C(46)           117.9(9)

C(42)-C(41)-P(4)            120.0(7)

C(46)-C(41)-P(4)            122.0(8)

C(41)-C(42)-C(43)           121.6(10)

C(44)-C(43)-C(42)           119.0(12)

C(43)-C(44)-C(45)           120.5(12)

C(44)-C(45)-C(46)           121.1(12)

C(41)-C(46)-C(45)           119.8(12)

C(52)-C(47)-C(48)           118.0(10)

C(52)-C(47)-P(4)            120.8(7)

C(48)-C(47)-P(4)            121.1(9)

C(47)-C(48)-C(49)           121.4(13)

C(50)-C(49)-C(48)           119.5(14)

C(49)-C(50)-C(51)           119.8(14)

C(52)-C(51)-C(50)           120.4(13)

C(51)-C(52)-C(47)           120.7(11)

O(2)-S(1)-O(1)              116.1(5)

O(2)-S(1)-O(3)              114.7(5)

O(1)-S(1)-O(3)              113.8(5)

O(2)-S(1)-C(53)             104.8(5)

O(1)-S(1)-C(53)             103.5(5)

O(3)-S(1)-C(53)             101.5(5)

F(2)-C(53)-F(3)             107.3(10)

F(2)-C(53)-F(1)             105.3(10)

F(3)-C(53)-F(1)             106.7(10)

F(2)-C(53)-S(1)             113.2(9)

F(3)-C(53)-S(1)             112.4(8)

F(1)-C(53)-S(1)             111.5(8)

O(6)-S(2)-O(4)              116.2(6)

O(6)-S(2)-O(5)              112.9(7)

O(4)-S(2)-O(5)              115.0(7)

O(6)-S(2)-C(54)             107.3(9)

O(4)-S(2)-C(54)             104.8(9)

O(5)-S(2)-C(54)              98.3(10)

F(5)-C(54)-F(4)             111(2)

F(5)-C(54)-F(6)             107(2)

F(4)-C(54)-F(6)             103.7(14)

F(5)-C(54)-S(2)             114.9(12)

F(4)-C(54)-S(2)             113(2)

F(6)-C(54)-S(2)             106(2)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

Table 4-2. Anisotropic displacement parameters (Å2×103) for 2. The anisotropic displacement factor exponent takes the form: -22[h2a*2U11 +  + 2hka*b*U12].

____________________________________________________________________________

U11        U22        U33        U23        U13        U12

____________________________________________________________________________

Pd(1)    29(1)      37(1)      33(1)      -2(1)       6(1)       2(1)

Pd(2)    31(1)      41(1)      33(1)      -1(1)       7(1)      -3(1)

P(1)     32(1)      39(1)      35(1)       1(1)       5(1)       0(1)

P(2)     37(1)      37(1)      41(1)       0(1)       9(1)       6(1)

P(3)     42(1)      48(1)      39(1)       2(1)      14(1)       1(1)

P(4)     34(1)      68(2)      36(1)       3(1)       6(1)      -7(1)

N(1)     35(4)      51(4)      40(4)       0(3)       6(3)       4(3)

N(2)     34(3)      44(4)      42(4)      -3(3)       4(3)       2(3)

C(1)     34(4)      48(5)      40(5)       8(4)      11(4)       1(4)

C(2)     66(6)      49(6)      47(5)       0(4)       5(4)       2(5)

C(3)     93(8)      38(5)      63(6)       6(5)      14(6)      11(5)

C(4)     58(6)      56(6)      75(7)      27(5)      12(5)      17(5)

C(5)     43(5)      74(7)      77(7)      26(6)     -11(5)      -6(5)

C(6)     41(5)      59(6)      62(6)      15(5)      -3(4)      -3(4)

C(7)     36(4)      40(5)      46(5)       3(4)       9(4)      -1(4)

C(8)     58(6)      48(5)      56(6)      -8(4)      19(5)     -12(4)

C(9)     71(7)      68(7)      71(7)       4(6)      36(6)     -13(6)

C(10)    46(5)      57(6)      94(8)       8(6)      25(5)      -4(5)

C(11)    44(5)      45(5)      87(8)      -1(5)       1(5)      -2(4)

C(12)    38(5)      49(5)      55(5)       1(4)       2(4)      -3(4)

C(13)    42(5)      59(5)      37(4)      -3(4)      11(4)      -1(4)

C(14)    46(5)      50(5)      50(5)      -9(4)      10(4)       7(4)

C(15)    44(5)      33(4)      47(5)       0(4)       6(4)       4(4)

C(16)    55(6)      63(6)      79(7)      31(5)      19(5)      14(5)

C(17)    87(8)      80(8)      82(8)      34(6)      31(6)       9(6)

C(18)    75(8)      72(7)      78(7)      30(6)       9(6)      27(6)

C(19)    57(6)     100(9)      90(8)      33(7)       6(6)      28(6)

C(20)    52(6)      76(7)      75(7)      23(6)      15(5)      24(5)

C(21)    43(5)      50(5)      41(5)       6(4)      14(4)       9(4)

C(22)    68(6)      55(6)      63(6)      -3(5)      27(5)      16(5)

C(23)    67(7)      97(9)      81(7)      25(7)      51(6)      35(6)

C(24)    68(7)      88(8)      84(8)      24(7)      38(6)       3(6)

C(25)    85(8)      59(6)      89(8)      -8(6)      44(6)     -21(6)

C(26)    58(6)      71(7)      57(6)      -6(5)      28(5)      -4(5)

C(27)    41(5)      59(6)      43(5)       2(4)      17(4)       0(4)

C(28)    65(7)      53(6)      88(7)      16(5)      20(6)       6(5)

C(29)    50(7)      94(9)     129(11)     26(8)      17(7)      16(6)

C(30)    46(6)     123(11)     79(8)       6(7)       9(5)      -2(7)

C(31)    55(7)     100(10)    113(10)     -9(8)      15(7)     -17(7)

C(32)    48(6)      72(7)      86(7)      -6(6)      18(5)      -2(5)

C(33)    45(5)      44(5)      47(5)       1(4)       6(4)       5(4)

C(34)    81(7)      52(6)      68(7)       2(5)      27(6)       1(5)

C(35)    92(8)      54(7)     107(10)      7(7)      25(7)      -8(6)

C(36)    88(9)      51(7)     108(10)    -12(7)      -3(7)      -5(6)

C(37)   128(11)     70(8)      91(9)     -33(7)      25(8)      -3(8)

C(38)    99(9)      77(8)      66(7)     -12(6)      31(6)      -5(6)

C(39)    52(5)      59(6)      51(5)       7(4)      21(4)       2(4)

C(40)    41(6)     218(15)     43(6)      38(7)      14(5)       3(7)

C(41)    33(4)      55(5)      52(5)      -1(4)       5(4)       0(4)

C(42)    63(6)      95(8)      67(7)     -17(6)      17(5)     -30(6)

C(43)    83(8)      85(8)      91(9)     -23(7)      20(7)     -37(7)

C(44)    65(8)      85(9)     136(13)    -25(9)      16(8)     -14(6)

C(45)   131(13)    135(14)     95(11)    -69(10)      8(9)     -34(11)

C(46)   111(10)    100(9)      55(7)     -22(6)       6(6)     -26(8)

C(47)    58(6)      47(5)      46(5)       5(4)      -4(4)      -9(4)

C(48)   110(10)     69(8)      86(8)     -10(6)      15(7)     -21(7)

C(49)   185(17)     53(8)     105(11)      1(7)       3(12)     -4(11)

C(50)   137(14)     86(11)     96(10)    -21(8)     -39(10)     38(11)

C(51)    76(8)      98(10)    102(10)    -20(8)      -9(7)      15(8)

C(52)    53(6)      57(6)      83(7)      -1(5)       3(5)       3(5)

S(1)     82(2)      45(1)      62(2)      -2(1)      28(1)      -4(1)

O(1)    120(6)      58(5)     106(6)     -29(4)      35(5)     -13(4)

O(2)    121(6)      54(4)      81(5)       5(4)      13(4)      32(4)

O(3)    109(6)      94(6)     104(6)       7(5)      54(5)     -27(5)

C(53)    78(8)      78(8)      78(8)       6(7)      31(6)      -1(6)

F(1)    132(6)     125(6)      74(4)     -20(4)      20(4)      -6(5)

F(2)    124(6)     217(10)    101(6)      -3(6)      63(5)     -52(6)

F(3)    173(8)     145(7)     104(6)      45(5)      39(5)      85(7)

S(2)    108(2)      67(2)      75(2)     -17(2)       3(2)       6(2)

O(4)     94(6)     144(8)      83(6)      -8(5)     -20(5)       0(6)

O(5)    197(12)    179(11)    105(8)      40(8)      49(8)     -22(9)

O(6)    308(16)     46(5)     139(9)     -21(5)     -61(9)       3(7)

C(54)    72(11)    112(14)    258(25)     -2(15)     26(14)    -21(9)

F(4)     82(7)     245(14)    386(22)     98(14)    -38(10)      1(8)

F(5)    191(12)    136(9)     423(22)   -133(12)     54(13)     37(9)

F(6)    169(12)    404(25)    283(19)    -27(17)    140(14)    -50(14)

____________________________________________________________________________

Table 5-2. Hydrogen coordinates (×104) and isotropic displacement parameters (Å2×103) for 2.

________________________________________________________________________

x             y             z           U(eq)

________________________________________________________________________

H(1A)        8365(5)       1665(2)       -283(5)       51

H(1B)        7577(5)       1416(2)        -59(5)       51

H(2A)       11078(5)       1430(2)        506(5)       49

H(2B)       11064(5)       1114(2)        960(5)       49

H(2)         7933(8)       1678(2)      -2342(8)       67

H(3)         6969(10)      2083(2)      -3464(8)       79

H(4)         5486(8)       1980(2)      -5137(9)       77

H(5)         4972(8)       1490(2)      -5657(9)       83

H(6)         5874(7)       1079(2)      -4531(8)       68

H(8)         7018(8)        865(2)       -394(8)       64

H(9)         5629(9)        544(2)         64(9)       80

H(10)        4568(8)        208(2)      -1360(10)      77

H(11)        4837(8)        218(2)      -3225(10)      73

H(12)        6200(7)        553(2)      -3701(8)       59

H(13A)       7977(7)        707(2)      -3982(7)       55

H(13B)       8950(7)        969(2)      -3823(7)       55

H(14A)       9989(7)        517(2)      -3167(7)       58

H(14B)       9113(7)        442(2)      -2357(7)       58

H(16)        9706(9)        471(2)        164(9)       78

H(17)       10572(10)       120(3)       1609(10)      97

H(18)       12601(10)        20(2)       2006(10)      92

H(19)       13766(10)       282(3)        965(10)     102

H(20)       12915(8)        612(2)       -514(9)       81

H(22)       12051(8)        650(2)      -2968(8)       72

H(23)       13602(9)        886(3)      -3557(9)       91

H(24)       14121(9)       1393(3)      -3023(10)      92

H(25)       13056(10)      1659(2)      -1924(9)       88

H(26)       11452(8)       1429(2)      -1375(8)       71

H(28)        6191(9)       2028(2)       2041(9)       82

H(29)        4156(10)      1964(3)       1137(12)     110

H(30)        3385(10)      1479(3)        771(10)     100

H(31)        4610(10)      1056(3)       1145(11)     108

H(32)        6639(8)       1125(2)       1980(9)       82

H(34)        9196(9)       2088(2)       1565(9)       79

H(35)        9921(10)      2568(2)       2041(12)     101

H(36)        9720(11)      2800(3)       3732(12)     105

H(37)        8785(12)      2541(3)       4986(12)     116

H(38)        8078(10)      2051(3)       4529(9)       94

H(39A)       8262(7)       1529(2)       4684(7)       63

H(39B)       8127(7)       1213(2)       4023(7)       63

H(40A)       9955(8)       1151(4)       4942(8)      120

H(40B)      10170(8)       1503(4)       5171(8)      120

H(42)       11742(9)       1788(3)       2131(9)       90

H(43)       12795(10)      2246(3)       2491(11)     104

H(44)       13383(11)      2425(3)       4357(15)     116

H(45)       12874(14)      2172(4)       5843(14)     148

H(46)       11869(11)      1710(3)       5518(10)     110

H(48)       10573(12)       739(3)       4151(10)     108

H(49)       11825(19)       315(3)       4424(13)     144

H(50)       13749(17)       362(4)       4193(13)     142

H(51)       14383(11)       823(3)       3578(11)     117

H(52)       13099(8)       1235(2)       3197(9)       80

________________________________________________________________________