Supplementary Information

Insight into surface and structural changes of Montmorillonite and Organo-montmorillonites loaded with Ag.

Alejandra M. Fernández Solarteab, Jhonny Villarroel-Rochac, César Fernández Morantesad, Maria L. Montese, Karim Sapagc, Gustavo Curutchetd and Rosa M. Torres Sáncheza(*)

aCETMIC-CCT La Plata-CIC, Camino Centenario y 506, (1897) M. B. Gonnet, La Plata, Argentina. bpresent address. Research group on Mechanical Desing and Material (GIDMyM), Univ. ECCI. Calle 51#19-12, Bogota DC, Colombia. cLaboratorio de Sólidos Porosos, INFAP-CONICET, Univ. Nacional de San Luis, Chacabuco 917, CP 5700, San Luis, Argentina. dLaboratorio de Análisis Ambiental, Instituto de Investigación e Ingeniería Ambiental. Univ. Nacional de San Martín, Av. 25 de Mayo y Francia, San Martin (1650), Buenos Aires, Argentina. eIFLP, Instituto de Física La Plata. CONICET-CCT-La Plata, Departamento de Física, Facultad de Ciencias Exactas, Universidad Nacional de La Plata, La Plata, Argentina.

Figure S1. FTIR of HDTMA and HDTMA-Ag complex in solution

{

Figure S2. SEM images: (A) MMT-Ag, (B) MH.5-Ag, (D) MH1-Ag and (D) MH2-Ag samples. Red circles evidence Ag aggregates.

| Element | Weight% | Atomic% |
| --- | --- | --- |
| O K | 49.94 | 63.85 |
| Mg K | 2.00 | 1.68 |
| Al K | 13.82 | 10.48 |
| Si K | 31.82 | 23.18 |
| Fe K | 1.99 | 0.73 |
| Ag L | 0.43 | 0.08 |
| Totals | 100.00 |  |

| Element | Weight% | Atomic% |
| --- | --- | --- |
| O K | 51.384 | 65.18 |
| Mg K | 1.85 | 1.54 |
| Al K | 12.85 | 9.67 |
| Si K | 32.09 | 23.19 |
| Fe K | 0.45 | 0.16 |
| Ag L | 1.39 | 0.26 |
| Totals | 100.00 |  |

Fig. S3. EDS elemental composition of samples MMT-Ag and MH0.5-Ag.

Figure S4. XRD patterns of indicated samples. Symbols indicated: () Ag0 and (*) AgBr.

Table S1. Dapp difference between the indicated samples

| Involved Samples | Dapp without Ag (nm) | Dapp with Ag (nm) |
| --- | --- | --- |
| MMT- MH0.5 | 539±61 | 428±29 |
| MH0.5- MH1 | 846±386 | 91±47 |
| MH1- MH2 | 789±471 | 1619±230 |